E.S.S. 7322/2011

Standards of Safety & Hygiene in Leather,

Leather Products & Parts

1. Scope

This Egyptian standard specification applies to the basic standards of safety and hygiene for leather, leather products and parts, whether components or final product. It also includes the methods of testing to verify such standards.

Note :

The product must pass the quality tests pursuant to its standard specifications.

2. Complementary Specifications

The following complementary references shall be used; noting that the latest edition of the reference would be applied (including any amendments).

2.1 EN ISO/TR 16178 Footwear - Critical substances

potentially present in footwear & footwear components.

2.2 EN 14362.1 Textiles - Methods for the determination of

certain aromatic amines derived from azo colorants.

Part 1 : Detection of the use of certain azo colorants

accessible without extraction.

2.3 EN 14362.2 Textiles - Methods for the determination of

certain aromatic amines derived from azo colorants.

Part 2 : Detection of the use of certain azo colorants

accessible by extracting the fibers.

2.4 EN 14362.3 Textiles - Methods for the determination of

certain aromatic amines derived from azo colorants.

Detection of the use of certain azo colorants which may

release 4-aminoazobenzene, accessible without

extraction.

4. Standards of Safety & Hygiene in Leather, Leather Products & Parts

4.1 Table 1 includes standards of safety & hygiene in leather, leather products &

parts

| Chemical Substances |  | Raw Material Used | Method of Testing | Limits Permitted |
| --- | --- | --- | --- | --- |
| 1. Rate of azo dye | Azo – aryl amines | Natural leather | EN/ISO 17234-1 | 1. The azo dye list and the Azo dye mentioned in Appendix 1 shall not be used in skin direct touching leather and textile substances. 2. Regarding the azo dye list mentioned in Appendix 2, they shall not be used in concentrations higher than 0.1% by weight as substances or mixtures to color textile and leather goods. |
|  | Azo – aryl amines When 4-aminoazobenzene is suspected | Natural leather | EN/ISO 17234-2 |  |
|  | Azo – aryl amines | - Synthetic leather : (polyamide – chloride fibers – polyaclyric) - Fabrics : (natural cellulose textile – natural protein textile) - Printed textiles | EN/ISO 14362-1 |  |
|  | Azo – aryl amines | - Printed textiles - Synthetic leather : polyester | EN/ISO 14362-2 |  |
|  | Azo – aryl amines When 4-aminoazobenzene is suspected | - Synthetic leather : (polyester – polyamide – chloride fibers – polyaclyric) - Fabrics : (natural cellulose textile – natural protein textile - Printed textiles | EN/ISO 14362-3 |  |

| Chemical Substances | Raw Material Used | Method of Testing | Limits Permitted |  |
| --- | --- | --- | --- | --- |
| 2. Cadmium (Cd) and compounds | - (Coated leather) - Synthetic leather - Printed textile | EN 1122 | Not more than 0.01% to polymer weight |  |
| 3. Rate of Chromium (VI) | Natural leather | EN ISO 17075 | Not more than 3 mg/kg |  |
| 4. Formaldehyde | Natural & synthetic leather | EN ISO 17226-1 Or ISO 17226-2 | Not more than 150 ppm. |  |
|  | Textile | EN ISO 14184-1 | Not more than 75 ppm. |  |
| 5. Heavy substances (Sb-As-Ba-Cd-Cr-Pb-Hg-Sc) | Children less than 36 months footwear (Size 26 & less) | EN 71-3 & ISO 17072-1 Or ISO 17072-2 | Element | Limit |
|  |  |  | Sb | Not more than 60 mg/kg in substance |
|  |  |  | As | Not more than 25 mg/kg in substance |
|  |  |  | Ba | Not more than 1000 mg/kg in substance |
|  |  |  | Cd | Not more than 75 mg/kg in substance |
|  |  |  | Cr | Not more than 60 mg/kg in substance |
|  |  |  | Pb | Not more than 90 mg/kg in substance |
|  |  |  | Hg | Not more than 60 mg/kg in substance |
|  |  |  | Sc | Not more than 500 mg/kg in substance |

| Chemical Substances | Raw Material Used | Method of Testing | Limits Permitted |
| --- | --- | --- | --- |
| 6. Nickel directly touching skin | Solid metal parts | EN 1811 CR 12471 EN 12472 | If the nickel dash is more than 0.5 mg/cm2/week, it shall not be used in units that directly touch the skin for a long period of time |
| 7. Content of pentachlorophenol (PCP), salts & esters | Natural leather | EN ISO 17070 | 1 ppm |
|  | Natural substances used in footwear manufacturing (lumber – cork) | EN/TR 14823 | Not more than 5 ppm |
|  | Fabrics (natural cellulose textile – natural protein textile) | XP-G 08 015/2000 | 1 ppm |
| 8. Rate of monomer in PVC | - Natural leather (coated leather) - Synthetic leather (polyvinylchloride) | ISO 6401 | Not more than 1 ppm |

| Chemical Substances | Raw Material Used |  | Method of Testing | Limits Permitted |
| --- | --- | --- | --- | --- |
| 9. Phthalates | In textile raw materials | In synthetic leather (PE-TP)-EVA-polyvinylchloride- rubber-all kinds of polyurethane | ISO 18856 | Not more than 0.1% by weight |
|  |  | - Coated leather - Synthetic leather (polyester-polyamide-chloride fibers-polyaclyric) - Fabrics (natural cellulose textile-natural protein textile) - Printed textile | EN 15777 | Not more than 0.1% by weight |
|  | Children less than 36 months footwear (Size 26 & less) | - Coated leather - Synthetic leather (polyester-polyamide-chloride fibers- polyaclyric-(PE-TP)-EVA-polyvinylchloride- rubber-all kinds of polyurethane) - Fabrics (natural cellulose textile-natural protein textile) - Printed textile | EN 71-10 & EN 71-11 | Not more than 0.1% by weight |